## Slide 1: 4D Printing from CFRP composites letter ‘S’
MECH 6521 – Manufacturing of composites
Course Instructor :- Dr. Suong Van Hoa
Yash Chauhan 40156647
Krushil Navadiya 40153144
Sahil Patel 40171642
Smit Kansagara 40184514
Bhargav Chavada 40186919
Aditya Kale. 40156585
Jagadeshwar Baskararaja 40198766
Belhanfnaout Mohamad Ali 40224122

## Slide 2: Scope of project
To manufacture letter "S" from Carbon Fiber Reinforced Polymer (CFRP) pre-pegs.
To manufacture letter "S" without using complex mold.
There’s neither any condition provided for any kind of load which needs to be bear by the structure nor any specific part dimension.

## Slide 3: Introduction
The technique used to make complex shapes without the use of a mold.
It is process that combines 3D printing with the application of some activating agent in order to change the shape of the manufactured part after the process.
Complex forms can be formed from flat surfaces, but the shape of final component (degree of cure) depends upon the type of manufacturing process and material used, orientation of fiber and hand lay-up sequence.
4-D printing is a technique similar to 3-D printing where the successive layer of deposited material gets deformed with time.
This characteristic can be exploited to create curved-geometry items without the usage of a complicated mold. Thus, it is also called as “Mold-less composites manufacturing".
4D Printing of Composites (4DPC) ?
This technique utilizes light weight, high strength, high stiffness composite materials that have been used to make light weight components

## Slide 4
Difference between 4DPC and Regular 4D printing ?
In regular 4D printing, the material used are usually soft polymeric materials, which have low stiffness (about 10GPa) and strength (about 10 MPa)
The materials (carbon/epoxy)used in 4DPC have high stiffness (about 100 GPa) and strength (about 100 MPa)
The principle of operation for 4DPC depends on the anisotropy of the laminate (which is made up of many layers with different fiber orientations).
Automated Fiber Placement :-
Used to deposit layers additively to produce stack of composites layers.

## Slide 5
Pre-peg
A fibrous material pre-impregnated with a particular synthetic resin, used in making reinforced plastics.
Properties of Carbon Fiber Reinfroced Polymers (CFRP)
Light Weight
High strength & stiffness
Good fatigue resistance

## Slide 6: Mechanism​
Mould less composites manufacturing : -​
Shape of symmetric laminates :- The symmetric laminates with layup sequence of [0/90]s or [0n/90n]s remains flat after curing and cooling to the room temperature.​
Shape of Unidirectional laminates :- Laminates in which substantially all the fibres are parallel are known as unidirectional laminates. Irrespective of any number of layers, these equally oriented laminas remain flat. ​
Shape of Cross ply laminates :- A cross-ply laminate is made up of an indefinite number of plies, each of which has a fiber orientation of 0° or 90° and can be symmetric or anti-symmetric.
Mechanisms :-
(1) Resin shrinkage
(2) Mismatch in coefficients of thermal contraction

## Slide 7: Composite Lay-Up
First Step -A layer with 0-degree orientation of length 25 Inch is initially placed on the tool. (Layer S).
Second Step - Afterwards, a 90-degree orientation layer is placed at the second elevation of the length 13 Inch over the layer S. (Layer A1).
Third Step - A same 90-degree layer of 13 Inch is placed over the layer A1 at third elevation from layer S. (Layer A2).​
Fourth Step - On the other side of the layer at the second elevation from the 0-degree orientation layer S, another layer of 90-degree orientation is laid of 13 Inch length. (Layer B1) ​
Fifth Step -Repeated third step over the layer B1 at third elevation from 0-degree orientation. (Layer B2).

## Slide 8
The segment AB corresponds to the unsymmetric laminate [0/902].
The segment DE corresponds to the unsymmetric laminate [902/0].
The region BCD is overlapped region BCD is straighter because the lay-up sequence in this segment is [902/0/902].

## Slide 9: Configuration of PART
Prepregs of Carbon Fiber reinforced Composites (CFRP)
Uniform Layers & Single Fiber direction (0° & 90°)
Total length before curing (24 inch)
1 layer of [0°] of 24 inches, and 4 layer of [90°] layers of 13 inches each.
1-inch-long overlap area
Reasons to take above specifications :-
Semi flat middle section area to emphasise the look of letter “S”
To avoid stress concentration point in which only 1 layer is cross-sectionally present

## Slide 10
Procedure
Steps :-
First protective film is removed.
Aluminum plate is cleaned using Acetone
Double Side tape is placed around the edge of the plate.
A release agent (Locktite 44 NC) is applied.
Composites laminates (Pre pegs) are placed on table
Bleeder layer
Breather layer

## Slide 11
Vacuum bag is placed, and holes are punched to install 2 valves (For autoclave & vacuum pump)
Vacuum bag sealed using Double sided tape (Air cannot leak)
Vacuum pump is engaged
Function of Non-stick Seperator :-
Prevent the bonding of two successive layers such as base layer and the laminate (Thin caul Plate)
Note :- Not used in our letter

## Slide 12: Curing cycle
A one-step (linear) increase in the autoclave temperature.
The autoclave is programmed to reach a maximum part temperature of 449.37 K.
Curing Temperature :- 177.7 °C
The maximum pressure programmed was 110.31 kPa.

## Slide 13: Results
Factors affecting the Final Part :-
The degree of shape changing depends on the material properties, the fiber orientation, the lay-up sequence and the manufacturing process.
The final part results can vary according to the amount of curing agent used with a particular type of resin which can create difference in the amount of shrinkage.
The properties of the final part are also dependent on the type, amount of resin, type of fiber and volume fraction of fiber.
As there is decrement in the temperature from cure temperature to the room temperature there is change in the modulus of the resin.

## Slide 14: Final Dimension of the part
Specific Dimension | Dimension (Cm)
Length | 45.20
Radius of Curvature | 11.30
Width | 11.30
Depth | 7.70
Ply Thickness | 0.0127

## Slide 15: Advantages ​
Inexpensive because complex mold is not required.
Manufacturing of curved shapes can be fast and economical
High manufacturing efficiency​
Reduced manufacturing cost and less carbon footprint​
Less space, less volume and lower labour cost​
Can resist harsh environmental conditions​
Structures may adapt and change in response to their surroundings​
4D printed structures reduces the component's weight by 80%​
Can simulate & predict the final configuration using Finite element analysis
Practical experience and knowledge required
Relatively low modulus as compared to 5D Printing
Less stable with environmental temperature
Complex structure and integrated parts manufacturing are complex
LIMITATIONS

## Slide 16: Application
4D printed materials are used in field of defence and protection which can change their shape according to environmental condition change
Aerospace industry
Automobile sector (Composites leaf spring)
Composites omega stiffeners
Robotics, Sensors & Flexible Electronics
Prostheses application in medical field
Space structures like satellites (PEEK)
Wind turbine blades & Sport equipment's
Architecture & Civil Infrastructure

## Slide 17: Future Scope
The concept of the pre-programmed intelligent object will appear to have multiple uses in various industries in the future.
The aerospace , automotive, healthcare and consumer sector are the final user.
Given the interests of manufacturers, this technology will make a faster exponential growth than projected.
In the future this technology will provide great ability to support complex items, long-term durable products and intelligent

## Slide 18
Anisotropic properties of composites can be used to make engineering structures.
The curvature of the composite part mainly be contingent on the asymmetric nature of laminate.
No need of any complex mold for manufacturing
The principle of 4D printing can be use successively to manufacture the composite parts with applicable strength and stiffness.
Upon curing and cooling it to the room temperature, curved laminate has been obtained.
conclusion

## Slide 19
Suong V. Hoa, Principles of the manufacturing of the composite materials, DEStech Publications, Inc, 2018
Suong V. Hoa, Factors affecting the properties of composites made by 4D printing (moldless composites manufacturing) 101-109
Suong V. Hoa, Development of composite springs using 4D printing methods
Suong Van Hoa (2017) Factors affecting the properties of composites made by 4D printing (moldless composites manufacturing), Advanced Manufacturing: Polymer & Composites Science, 3:3, 101-109, DOI: 10.1080/20550340.2017.1355519
https://www.4dpmmconference.com/speaker/4d-printing-of-composites/
https://3dprintingindustry.com/news/concordia-4d-printing-makes-moldless-composites-faster-cheaper-131469/
https://www.youtube.com/watch?v=JQPHCqaBzCw
References

## Slide 20: Thanks for your time and attention we are open to questions
Click to add text